## Slide 1
ACCL23-12 Interview
Presenter: Eric Viklund

## Slide 2: Personal Introduction
Name: Eric Viklund
Contact:
  ericviklund2023@u.northwestern.edu
  +1(860)834-5008
Education:
  B.S. Physics from University of Connecticut
  Currently PhD candidate at Northwestern University
Publications
  Viklund, Eric, et al. Superconductor Science and Technology 37.2 (2024): 025009.
  Viklund, Eric, et al. APL Materials 12.7 (2024).
  Viklund, E., et al. IEEE Transactions on Applied Superconductivity 33.5 (2023): 1-4.
  Viklund, Eric, et al. No. FERMILAB-CONF-22-825-TD. Fermi National Accelerator Lab.(FNAL), Batavia, IL (United States), 2022.

## Slide 3: Outline
Research Experience
  Study on the Electrochemical Polishing Process Applied to Niobium SRF Cavities
  Development of a Mechanical Polishing Process for Nb3Sn Coated SRF Cavities
  Development of a New Recoating Procedure to Heal Nb3Sn Cavities.
Research Proposal
  Cost Reduction Methods for Niobium SRF Cavity Fabrication
    Study on the HF-Free Bipolar Electrochemical Polishing Method

## Slide 4: Electropolishing Study
Etching and pitting sometimes occur in nitrogen doped niobium cavities.
A better understanding of EP necessary to understand and prevent these defects.
Sample study to test different polishing parameters.
  Applied voltage
  Electrolyte temperature
  Nitrogen doping

## Slide 5: Surface Analysis of Electropolished Samples
Etching was caused by low polishing voltage.
  Nitrogen doping shows no effect on etching.
  Temperature has no direct impact but can cause an ohmic voltage drop in the electrolyte due to high currents.
Increased voltage and cathode surface area required to prevent etching.
0.5
0.6
0.7
0.8
0.9
1.0
1.1
1.2
Voltage
Undoped
Nitrogen Doped
Nitrogen Doped Cold EP
0.5
0.6
0.7
0.8
0.9
1.0
1.1
1.2
Voltage
Undoped
Nitrogen Doped
Nitrogen Doped Cold EP

## Slide 6: Electrochemical Impedance Spectroscopy
Electrochemical impedance spectroscopy (EIS)
  A small alternating voltage is applied.
  Electrical impedance spectrum is measured.
Impedance spectrum gives information on the chemical processes on the electrode.
How do we interpret this data?

## Slide 7: Data Analysis Using Distribution of Relaxation Times Fitting
Distribution of Relaxation Times
  Calculate the relaxation time of different surface processes.
Three distinct relaxation times
  Double layer capacitance
  Low voltage NbO oxidation peak
  High voltage Nb2O5 oxidation peak

## Slide 8: Nb2O5 Oxidation Effect on Surface Finish
0.5
0.6
0.7
0.8
0.9
1.0
1.1
1.2

## Slide 9: Beyond Niobium – Nb3Sn Thin Film Cavities
 | Nb | Nb3Sn | Difference
Q@4K,1.3GHz | ~109 |  | 
Emax | 50 MV/m |  | 

## Slide 10: Beyond Niobium – Nb3Sn Thin Film Cavities
 | Nb | Nb3Sn | Difference
Q@4K,1.3GHz | ~109 | ~1010 | 10x
Emax | 50 MV/m | 100 MV/m | 2x

## Slide 11: Beyond Niobium – Nb3Sn Thin Film Cavities
 | Nb | Nb3Sn | Difference
Q@4K,1.3GHz | ~109 | ~1010 | 10x
Emax | 50 MV/m | ~20 MV/m | 2x

## Slide 12: Challenges of Nb3Sn Cavity Fabrication
Nb3Sn is deposited by Sn vapor-diffusion.
Stoichiometry is important.
Nb3Sn too thin to be electropolished.
Lee, Jaeyel, et al. Superconductor Science and Technology 32.2 (2018): 024001.
3 μm
  Viklund, Eric, et al. Superconductor Science and Technology 37.2 (2024): 025009.

## Slide 13: Investigation of Sn Deficient Regions Using 3D Tomography
Bulk Nb
Nb3Sn
Pt Cap
X
Y
Z
Viklund, E., et al. IEEE Transactions on Applied Superconductivity 33.5 (2023): 1-4.

## Slide 14: Combined 3D EDS and EBSD
EDS shows Sn distribution within the film.
EBSD shows the grain structure of the film.
Sn deficient are shown to be intra granular as suggested by the Sn nucleation model.

## Slide 15: Centrifugal Barrel Polishing (CBP)

## Slide 16: Nb3Sn Sample Polishing Using a Coupon Cavity
Internal View
1 cm Nb3Sn coated sample

## Slide 17
86 μm
0 hours
2 hours
4 hours
6 hours
8 hours
  Viklund, Eric, et al. Superconductor Science and Technology 37.2 (2024): 025009.

## Slide 18
Initial Surface
2 hours
4 hours
6 hours
8 hours
5 μm
5 μm
5 μm
5 μm
5 μm
  Viklund, Eric, et al. Superconductor Science and Technology 37.2 (2024): 025009.

## Slide 19: Nanoscale Image of a Polished Nb3Sn Thin Film
Nb3Sn
Nb3Sn
Oxide Layer
Oxide Layer
Pt Cap
Pt Cap
  Viklund, Eric, et al. Superconductor Science and Technology 37.2 (2024): 025009.

## Slide 20: CBP Surface Roughness and Removal Rate
Chart: Duration of CBP[hours]
| 0 | 2 | 6 | 8
 | 3.104 | 2.796 | 1.952 | 1.826
Chart: Duration of CBP [hours]
| 0 | 2 | 4 | 6 | 8
Polished Nb3Sn | 208.2381 | 185.1343 | 100.2737 | 54.2454 | 16.5368
~170 nm/hr
Typical Niobium Cavity
  Viklund, Eric, et al. Superconductor Science and Technology 37.2 (2024): 025009.

## Slide 21: Applying Centrifugal Barrel Polishing (CBP) to a Nb3Sn Cavity
Before Nb3Sn Coating
After Nb3Sn Coating
After Polishing
Nb3Sn
4-hour CBP

## Slide 22: Performance of a Mechanically Polished Nb3Sn SRF Cavity
Polishing initially causes degradation.
A second coating is applied to fix the degradation.
Max accelerating field increases.
  10 MV/m to 14 MV/m
Quality factor stays the same.
First successful application of mechanical polishing to a Nb3Sn cavity!
  Viklund, Eric, et al. Superconductor Science and Technology 37.2 (2024): 025009.

## Slide 23: Recoating Heals Degraded Nb3Sn Cavities
A second, light coating is required to improve performance.
  1100 ℃ → 1000 ℃
  5 h → 1 h
  4 g of Sn → 0.85 g of Sn
Nb3Sn cavity performance is degraded by strain.
  Tuning
  Assembly
  Transportation

## Slide 24: Recoated Cavity T-Map
Degraded cavity equator hotspot.
Recoating heals the defect causing the hotspot.

## Slide 25: Finding the Mechanism of Nb3Sn Cavity Healing
Strain applied to cavity causes cracks in Nb3Sn coating.
Somehow the recoating can repair cracks.
  Are the cracks being filled in?
  Is the Nb3Sn coating re-dissolving?
  Is the new Nb3Sn stoichiometric?
Nb3Sn coated wires are used to study crack formation and healing.
  0.1% to 0.5% elongation of the wire causes crack formation.

## Slide 26: Results of Wire Study
New Nb3Sn is formed in the crack and at the base of the crack in the Nb substrate.
New material is stoichiometric.

## Slide 27
Eric Viklund
Research Proposal:
SRF Cavity Manufacturing Cost Reduction

## Slide 28: HF-Free Bipolar Electropolishing
HF-based EP
  Environmental impact.
  Human safety risk.
  Increased costs.
Cost estimates for electropolishing with HF is $2,934 per cavity.1
Polishing occurs through alternating anodic and cathodic pulses.
Bipolar EP
  No HF required.
  Neutral, non-toxic electrolyte
  Cheaper
Tian, Hui, and Charles Reece. No. JLAB-ACC-19-3164; DOE/OR/23177-6266. Thomas Jefferson National Accelerator Facility (TJNAF), Newport News, VA (United States), 2019.

## Slide 29: Bipolar Electropolishing Study
Bipolar EP has been shown to be effective by Faraday Technology, Inc., Cornell SRF group, KEK, and Jefferson Lab.
Removal rate is too slow.
  120 hours to remove 64 μm1
Removal rates are limited by power supply.
  High currents during voltage pulse
  Limited repetition rate
F. Furuta et al., in Proc. 18th Int. Conf. on RF Superconductivity (SRF'17), Lanzhou, China, July 2017, paper TUPB074, pp. 567-570, ISBN: 978-3-95450-191-5, https://doi.org/10.18429/JACoW-SRF2017-TUPB074, 2018.
Tian, Hui, et al. No. JLAB-ACC-18-2836; DOE/OR/23177-4574; TUPO043. Thomas Jefferson National Accelerator Facility (TJNAF), Newport News, VA (United States), 2019.

## Slide 30: Plan of Study
Understand the Bipolar EP Chemical Mechanism
  Electrochemical impedance spectroscopy
  Sample study
Optimize the parameters of the bipolar EP based on new knowledge.
  Higher removal rates.
  Safe, neutral electrolyte
Utilize KEK’s vertical EP capabilities to develop a new multi-cell capable power supply.
  High current density
  High repetition rate

## Slide 31: Research Experience
Material Analysis
  HR-TEM
  FIB/SEM
  3D EDS/EBSD
Electrochemistry
  Electrochemical impedance spectroscopy
  Complex data analysis
SRF Technology
  Cavity testing
  Nb3Sn coating
  Electropolishing and Mechanical polishing
Publications
  Viklund, Eric, et al. Superconductor Science and Technology 37.2 (2024): 025009.
  Viklund, Eric, et al. APL Materials 12.7 (2024).
  Viklund, E., et al. IEEE Transactions on Applied Superconductivity 33.5 (2023): 1-4.
  Viklund, Eric, et al. No. FERMILAB-CONF-22-825-TD. Fermi National Accelerator Lab.(FNAL), Batavia, IL (United States), 2022.