## Slide 1
ACCL23-12 Interview
Presenter: Eric Viklund

## Slide 2: Personal Introduction
Name: Eric Viklund
Contact:
  ericviklund2023@u.northwestern.edu
  +1(860)834-5008
Education:
  B.S. Physics from University of Connecticut
  Currently PhD candidate at Northwestern University
Research Experience:
  SRF Cavity Manufacturing Technology
    Electropolishing
    Mechanical Polishing
    Nb3Sn Cavity Manufacturing via Tin Vapor Diffusion
  Surface Analysis
    Scanning and Tunneling Electron Beam Microscopy
    Focused Ion Beam Milling for Sample Preparation and 3D Imaging

## Slide 3: Outline
Research Experience
  Study on the Electrochemical Polishing Process Applied to Niobium SRF Cavities
  Development of a Mechanical Polishing Process for Nb3Sn Coated SRF Cavities
Research Proposal
  Cost Reduction Methods for Niobium SRF Cavity Fabrication
    Study on the Mechanical Properties of Large Grain Niobium and the Deep Drawing Fabrication Method
    Study on the HF-Free Bipolar Electrochemical Polishing Method

## Slide 4: Electropolishing Study
Defects such as etching and pitting were discovered in nitrogen doped niobium cavities.
It was determined that a better understanding of EP was necessary to understand and prevent these defects.
Niobium samples are electropolished using different parameters.
  Applied voltage
  Electrolyte temperature
  Nitrogen doping

## Slide 5: Surface Analysis of Electropolished Samples
The sample study showed that the etching was caused by low polishing voltage.
Nitrogen doping shows no effect on etching.
Temperature has no direct impact but can cause an ohmic voltage drop in the electrolyte due to high currents.
Cathode was redesigned and voltage increased to prevent etching in cavities.
0.5
0.6
0.7
0.8
0.9
1.0
1.1
1.2
Voltage
Undoped
Nitrogen Doped
Nitrogen Doped Cold EP
0.5
0.6
0.7
0.8
0.9
1.0
1.1
1.2
Voltage
Undoped
Nitrogen Doped
Nitrogen Doped Cold EP

## Slide 6: Electrochemical Impedance Spectroscopy
To understand the cause of etching in cavities, electrochemical impedance spectroscopy (EIS) can provide more information on the chemical processes on the electrode surface.
A small alternating voltage is applied to the electrode to measure the complex electrical impedance spectrum.
This spectrum can show how the surface chemistry changes for different applied voltages.
The real (top) and imaginary (bottom) components of the complex electrical impedance of a niobium electrode during room temperature electropolishing at applied voltages ranging from 0.5 to 0.9 volts.

## Slide 7: Data Analysis Using Distribution of Relaxation Times Fitting
The distribution of relaxation times de-convolves the impedance spectrum revealing distinct peaks that correspond to chemical processes.
At low voltage only the electric double layer contributes to the impedance.
As the voltage is increased a second contribution from the oxide film is measured.
The oxide film contribution develops further indicating the transition from a thin partial oxide layer to a thick oxide layer.

## Slide 8: Nb3Sn Polishing Using Centrifugal Barrel Polishing
Internal View
Nb3Sn films have a rough surface that can enhance magnetic fields and reduce cavity performance.
Chemical polishing methods are not suitable.
Mechanical polishing was analyzed as an alternative using a coupon cavity sample study.

## Slide 9: Surface Profile after Progressing Amounts of Mechanical Polishing
86 μm
0 hours
2 hours
4 hours
6 hours
8 hours

## Slide 10: Scanning Electron Microscopy of Mechanically Polished Nb3Sn Films
Initial Surface
2 hours
4 hours
6 hours
8 hours
5 μm
5 μm
5 μm
5 μm
5 μm

## Slide 11: Surface Roughness of Mechanically Polished Nb3Sn Films
Mirror-like surface finish
10x reduction in surface roughness after 8 hours of tumbling
As-coated Nb3Sn
Nb3Sn after polishing
Pudasaini, Uttar, et al. Proceedings of the 18th International Conference on RF Superconductivity,(Lanzhou, China). 2017.
Chart: Duration of Centrifugal Barrel Polishing [hours]
| 0 | 2 | 4 | 6 | 8 | 10
Shiny Nb3Sn Films | 63 | 63 | 63 | 63 | 63 | 63
Polished Nb3Sn | 208.2381 | 185.1343 | 100.2737 | 54.2454 | 16.5368
Electropolished Nb | 25 | 25 | 25 | 25 | 25 | 25
Mechanical Polishing
Electropolishing

## Slide 12: Applying the Polishing Procedure to a Nb3Sn SRF Cavity
Mechanical polishing was tested on a Nb3Sn-coated single cell 1.3GHz cavity
4 hours of centrifugal barrel polishing
30 minutes of cleaning in an ultrasonic cleaner
Rinsed with a high-pressure (100 bars) water jet
Before Coating
After Coating
After Polishing

## Slide 13: Performance of a Mechanically Polished Nb3Sn SRF Cavity
Chart: Accelerating Field [MV/m]
| 3.45570098 | 3.8700926299999998 | 1.9977665200000001 | 2.5521534699999999 | 2.64058306 | 2.8837723799999999 | 3.10438473 | 3.2500463000000002 | 3.3882005899999998 | 3.4518109400000001 | 3.4940330300000002 | 3.5864713699999999 | 3.66369853 | 3.7512297700000001 | 4.0281081199999997 | 4.3218990000000002 | 4.7009263600000004 | 5.02610183 | 5.3563728900000003 | 5.6734349999999996 | 5.99472132 | 6.1770229199999998 | 3.9526751199999999 | 6.5977004499999996 | 6.31940043 | 6.7899929700000001 | 6.9945055600000003 | 7.3554155200000002 | 7.6864754 | 8.0091962399999996 | 8.0240256500000005 | 8.2002826399999993 | 8.53553563 | 8.9773552999999993 | 9.4608237000000006 | 4.9009713699999997 | 9.6072569600000008 | 9.1547189800000002 | 9.4015992799999992 | 9.6671483400000007 | 9.9260604099999998 | 10.2420866 | 10.124867200000001
4.4K Before CBP | 23143361800 | 17876552000 | 22694270600 | 23161525600 | 23730945600 | 23545774900 | 23279796400 | 22994580600 | 22515254300 | 21903820100 | 21280212000 | 20123231400 | 19384594500 | 18477556300 | 16851239400 | 15837371900 | 15081005700 | 14631380100 | 14035298100 | 13713888500 | 13340831400 | 13150935800 | 17112939300 | 12719182900 | 13003548000 | 12464559200 | 12062238800 | 11700599800 | 11185132700 | 10200146600 | 10167109800 | 9840167550 | 9408361320 | 9019511540 | 8879178480 | 7209223780 | 8913762610 | 7953843030 | 7814778150 | 7696339690 | 7454509490 | 7012311440 | 6979552200
2.0K Before CBP | 45095644400 | 46484829700 | 71461836000 | 85445202800 | 88339240400 | 88541070400 | 92012738500 | 99301364300 | 91030691000 | 96299315700 | 98262788800 | 103191781000 | 92831887500 | 87943381400 | 87230858700 | 90657287300 | 90988377100 | 89840295000 | 84925707300 | 87256408100 | 87564657200 | 88745309200 | 88992755600 | 83874114800 | 85064715700 | 79181977900 | 79282055600 | 72817731700 | 63959415800 | 63442611100 | 63542541500 | 56005029700 | 48550250000 | 40455401300 | 40440659500 | 40475072600 | 34124321000 | 30777565200 | 27640917800 | 25152986900 | 23528166800 | 22279459200 | 21231285100 | 20177108700 | 19142780900 | 18115254600 | 17491373800 | 17375644400 | 17432706600
4.4K After CBP | 8888103050 | 6124229210 | 11562833800 | 15134986100 | 26790143800 | 14748894300 | 14214412400 | 12809013500 | 12374153200 | 10621486300 | 9997664290 | 7873096380 | 6230390840 | 5653022900 | 4982955190 | 4855981510 | 13770187000 | 14555745500 | 15075026000 | 16048949100 | 15454593300 | 16371005300 | 16620094400 | 16718867300 | 17153334000 | 5390979330 | 4345842820 | 3185101230 | 2785249360 | 2128848540 | 1714609750 | 1193970430 | 1042184260 | 749205156 | 493896754 | 444171324 | 621914290 | 712920846 | 848299685 | 1114382760 | 1249446520 | 1940479700 | 2471535870 | 2618332770 | 3069214360 | 3272904330 | 4238431800 | 6511286750 | 7424318600 | 7601897300 | 7723080620 | 8054398830 | 8480470790 | 9471353580 | 9651469290 | 9940289670 | 10659994800 | 10488475200
4.4K After Recoating | 13549034100 | 14490202400 | 15155108900 | 15741471300 | 15934257400 | 16203255500 | 17463718100 | 12739214800 | 16328675900 | 12013323600 | 10759041500 | 9695374690 | 9192853540 | 8822941370 | 8483547310 | 7733551730 | 6848713810 | 6467975200 | 6008511460 | 5404843260 | 5008149100 | 4517545080 | 4236092410 | 3665740800 | 3213458930 | 2860964800 | 2765500390 | 2339782370 | 1937958460 | 1714042080 | 12666161900
2.0K After Recoating | 89639638200 | 90069199400 | 91330637700 | 94993579000 | 97799182900 | 100300726000 | 95148210100 | 96065880800 | 85981226400 | 80980848600 | 75942732000 | 67089195000 | 59352527000 | 52461645000 | 42774549500 | 36662803400 | 28704526600 | 22674466900 | 17999670200 | 13531589100 | 10642362600 | 8267954340 | 6574776360 | 4037331730 | 3991369050
Cavity performance was degraded after CBP.
A recoating was applied to the cavity to repair the damage.
After recoating, performance was significantly improved over the unpolished cavity.
Typical Nb Q at 4K

## Slide 14: Temperature Mapping and Sample Cutout Study
The temperature distribution over the surface of the cavity was measured using an array of sensors.
Two potential quench locations can be seen.
The hot spots were cut from the cavity and analyzed to determine the quench mechanism.
Several cold spots were cut from the cavity to compare.

## Slide 15: Cross-Section EDS Analysis of Cutouts
Bulk Nb
Nb3Sn
Pt Cap
X
Y
Z
The Composition of the film is measured using EDS in 3D by a FIB-SEM instrument.
The film contains many Sn deficient regions especially near the Nb3Sn-Nb interface.
Aluminum-oxide particles can be seen on the surface of the film.

## Slide 16
Eric Viklund
Research Proposal:
SRF Cavity Manufacturing Cost Reduction

## Slide 17: Overview
Niobium SRF cavities contribute significantly to the overall cost of the cryomodule
Each 9-cell niobium cavity costs ~$100,000
Additional treatments further increase costs
  Surface polishing
  Doping and heat treatments
To reach the ~900 cryomodules required for the ILC, costs must be reduced
Two cost saving technologies:
  Large grain SRF cavity fabrication
  HF-free electropolishing

## Slide 18: Study on Deformation and Annealing Properties of Large Grain Niobium
Large grain niobium is an attractive material for SRF cavities due to lower cost compared to fine grain niobium.
  Disks are cut directly from ingot
  No forging and annealing of the niobium sheet required
  Lower material waste generated, 15% compared to 45%1
Fabrication is more difficult compared to fine grain niobium
  Anisotropic material properties
  Weakness at grain boundaries
To improve the large grain cavity fabrication process, I will study the annealing and deformation properties of large grain niobium.
1. Kneisel, P., et al. Nuclear Instruments and Methods in Physics Research Section A: Accelerators, Spectrometers, Detectors and Associated Equipment 774 (2015): 133-150.

## Slide 19: Current Issues with Large Grain Niobium Cavity Fabrication
Manufacturing defects are more common in LG cavities due to anisotropic material properties.
  Oval shaped cavities
  Grain boundary slippage
  Non-uniform thickness
These defects compromise the cavity structural integrity and dimensional accuracy.
1. Kneisel, P., et al. Nuclear Instruments and Methods in Physics Research Section A: Accelerators, Spectrometers, Detectors and Associated Equipment 774 (2015): 133-150.

## Slide 20: Annealing
Annealing the niobium increases the ductility of the material by allowing for dislocation motion.
Ductility is improved through two processes:
  Grain nucleation
  Recovery
Intermediate annealing already used for cavity fabrication with hydroforming to improve the ductility of fine grain niobium.1
By introducing an annealing step during the deep drawing of the cavity, the manufacturing defects could be reduced or eliminated.
https://en.wikipedia.org/wiki/Recovery_(metallurgy)
1. Yamanaka, Masashi, et al. THPB041,(these proceedings), SRF2015, Whistler, Canada (2015).

## Slide 21: Plan of Study
Mechanical property study using large grain test samples.
  Anisotropic mechanical properties
  Grain boundary properties
Study annealing properties in sample using furnace.
  Recrystallization and recovery
  Ductility
Model behavior of large grain niobium during cavity drawing using computational modelling.
Apply findings to large grain cavity fabrication process.
This study will utilize the press forming and high temperature furnace capabilities of KEK’s Cavity Fabrication Facility.

## Slide 22: HF-Free Bipolar Electropolishing
The use of HF in the fabrication of niobium SRF cavities provides a challenge for the large-scale production of cavities.
  Environmental impact of large volumes of toxic chemicals used.
  Human safety risk of working with toxic chemicals.
  Increased costs due to strict safety requirements and procedures.
Cost estimates for electropolishing with HF is $2,934 per cavity.1
1. Taylor, E. J., et al. SRF2015, Whistler, BC, Canada (2015): 359.
Bipolar electropolishing is a new technique for polishing niobium without using HF acid.
Material removal is achieved by alternating the polarity of the niobium.
  Anodic oxidation pulse
  Cathodic dissolution of the oxide
Bipolar electropolishing can utilize HF-free electrolytes or even neutral salt-based electrolytes.

## Slide 23: Bipolar Electropolishing Study
Bipolar EP has been shown to be effective by Faraday Technology, Inc., Cornell SRF group, KEK, and Jefferson Lab.
To integrate bipolar electropolishing in large-scale cavity fabrication for the ILC the removal rate must be improved.
  120 hours to remove 64 μm1
Removal rates are currently limited by the power supply.
  High currents during voltage pulse
  Electrolysis during cathodic pulse
  Limited repetition rate
F. Furuta et al., in Proc. 18th Int. Conf. on RF Superconductivity (SRF'17), Lanzhou, China, July 2017, paper TUPB074, pp. 567-570, ISBN: 978-3-95450-191-5, https://doi.org/10.18429/JACoW-SRF2017-TUPB074, 2018.
Tian, Hui, et al. No. JLAB-ACC-18-2836; DOE/OR/23177-4574; TUPO043. Thomas Jefferson National Accelerator Facility (TJNAF), Newport News, VA (United States), 2019.

## Slide 24: Plan of Study
Optimize bipolar EP parameters through a sample study
  Optimize pulse waveform for high efficiency
  Explore different electrolytes, neutral salt electrolytes
Electrochemical impedance spectroscopy will be used to analyze the electrochemical nature of the process to better determine the optimal pulse voltage and duration.
Utilize KEK’s vertical EP capabilities and develop high current pulsed power supply to perform bipolar EP on 1-cell and 9-cell cavities.

## Slide 25: Questions