## Slide 1
ACCL23-12 Interview
Presenter: Eric Viklund

## Slide 2: Personal Introduction
Name: Eric Viklund
Contact:
  ericviklund2023@u.northwestern.edu
  +1(860)834-5008
Education:
  B.S. Physics from University of Connecticut
  Currently PhD candidate at Northwestern University
Research Experience:
  SRF Cavity Manufacturing Technology
    Electropolishing
    Mechanical Polishing
    Nb3Sn Cavity Manufacturing via Tin Vapor Diffusion
  Surface Analysis
    Scanning and Tunneling Electron Beam Microscopy
    Focused Ion Beam Milling for Sample Preparation and 3D Imaging

## Slide 3: Outline
Research Experience
  Study on the Electrochemical Polishing Process Applied to Niobium SRF Cavities
  Development of a Mechanical Polishing Process for Nb3Sn Coated SRF Cavities
Research Proposal
  Cost Reduction Methods for Niobium SRF Cavity Fabrication
    Study on the HF-Free Bipolar Electrochemical Polishing Method

## Slide 4: Electropolishing Study
Defects such as etching and pitting were discovered in nitrogen doped niobium cavities.
It was determined that a better understanding of EP was necessary to understand and prevent these defects.
Niobium samples are electropolished using different parameters.
  Applied voltage
  Electrolyte temperature
  Nitrogen doping

## Slide 5: Surface Analysis of Electropolished Samples
The sample study showed that the etching was caused by low polishing voltage.
Nitrogen doping shows no effect on etching.
Temperature has no direct impact but can cause an ohmic voltage drop in the electrolyte due to high currents.
Cathode was redesigned and voltage increased to prevent etching in cavities.
0.5
0.6
0.7
0.8
0.9
1.0
1.1
1.2
Voltage
Undoped
Nitrogen Doped
Nitrogen Doped Cold EP
0.5
0.6
0.7
0.8
0.9
1.0
1.1
1.2
Voltage
Undoped
Nitrogen Doped
Nitrogen Doped Cold EP

## Slide 6: Electrochemical Impedance Spectroscopy
To understand the cause of etching in cavities, electrochemical impedance spectroscopy (EIS) can provide more information on the chemical processes on the electrode surface.
A small alternating voltage is applied to the electrode to measure the complex electrical impedance spectrum.
This spectrum can show how the surface chemistry changes for different applied voltages.

## Slide 7: Data Analysis Using Distribution of Relaxation Times Fitting
The distribution of relaxation times de-convolves the impedance spectrum revealing distinct peaks that correspond to chemical processes.
At low voltage only the electric double layer contributes to the impedance.
As the voltage is increased a second contribution from the oxide film is measured.
The oxide film contribution develops further indicating the transition from a thin partial oxide layer to a thick oxide layer.

## Slide 8: Quantifying SRF Cavity Performance
Two major performance metrics:
  Quality Factor
  Accelerating Field
    Limited by superheating field Hsh.
Hsh

## Slide 9: Beyond Niobium – Nb3Sn Thin Film Cavities
 | Nb | Nb3Sn | Difference
Q@4K | ~109 |  | 
Emax | 50 MV/m |  | 

## Slide 10: Beyond Niobium – Nb3Sn Thin Film Cavities
 | Nb | Nb3Sn | Difference
Q@4K | ~109 | ~1010 | 10x
Emax | 50 MV/m | 100 MV/m | 2x

## Slide 11: Beyond Niobium – Nb3Sn Thin Film Cavities
 | Nb | Nb3Sn | Difference
Q@4K | ~109 | ~1010 | 10x
Emax | 50 MV/m | ~20 MV/m | 2x

## Slide 12: Challenges of Nb3Sn Cavity Fabrication
Nb3Sn is brittle.
Stoichiometry is important.
Nb3Sn cannot be electropolished.
Lee, Jaeyel, et al. Superconductor Science and Technology 32.2 (2018): 024001.
3 μm
  Viklund, Eric, et al. Superconductor Science and Technology 37.2 (2024): 025009.

## Slide 13: Investigation of Sn Deficient Regions Using 3D Tomography
Bulk Nb
Nb3Sn
Pt Cap
X
Y
Z
Viklund, E., et al. IEEE Transactions on Applied Superconductivity 33.5 (2023): 1-4.

## Slide 14: Combined 3D EDS and EBSD
EDS shows Sn distribution within the film.
EBSD shows the grain structure of the film.
Sn deficient are shown to be intra granular as suggested by the Sn nucleation model.

## Slide 15: Centrifugal Barrel Polishing (CBP)

## Slide 16: Nb3Sn Sample Polishing Using a Coupon Cavity
Internal View
1 cm Nb3Sn coated sample

## Slide 17
86 μm
0 hours
2 hours
4 hours
6 hours
8 hours
  Viklund, Eric, et al. Superconductor Science and Technology 37.2 (2024): 025009.

## Slide 18
Initial Surface
2 hours
4 hours
6 hours
8 hours
5 μm
5 μm
5 μm
5 μm
5 μm
  Viklund, Eric, et al. Superconductor Science and Technology 37.2 (2024): 025009.

## Slide 19: Nanoscale Image of a Polished Nb3Sn Thin Film
Nb3Sn
Nb3Sn
Oxide Layer
Oxide Layer
Pt Cap
Pt Cap
  Viklund, Eric, et al. Superconductor Science and Technology 37.2 (2024): 025009.

## Slide 20: CBP Surface Roughness and Removal Rate
Chart: Duration of CBP[hours]
| 0 | 2 | 6 | 8
 | 3.104 | 2.796 | 1.952 | 1.826
Chart: Duration of CBP [hours]
| 0 | 2 | 4 | 6 | 8
Polished Nb3Sn | 208.2381 | 185.1343 | 100.2737 | 54.2454 | 16.5368
~170 nm/hr
Typical Niobium Cavity
  Viklund, Eric, et al. Superconductor Science and Technology 37.2 (2024): 025009.

## Slide 21: Applying Centrifugal Barrel Polishing (CBP) to a Nb3Sn Cavity
Before Nb3Sn Coating
After Nb3Sn Coating
After Polishing
Nb3Sn
4-hour CBP

## Slide 22: Performance of a Mechanically Polished Nb3Sn SRF Cavity
Polishing initially causes degradation.
A second coating is applied to fix the degradation.
Max accelerating field increases.
  10 MV/m to 14 MV/m
Quality factor stays the same.
First successful application of polishing to a Nb3Sn cavity!
  Viklund, Eric, et al. Superconductor Science and Technology 37.2 (2024): 025009.

## Slide 23: Recoating Heals Degraded Nb3Sn Cavities
Nb3Sn cavity performance is degraded by strain.
  Tuning
  Assembly
  Transportation
A second, light coating is required to fix performance.
  1200 ℃ → 1000 ℃
  5 h → 1 h
  4 g of Sn → 0.85 g of Sn

## Slide 24: Recoated Cavity T-Map
Degraded cavity equator hotspot.
Recoating heals the defect causing the hotspot.

## Slide 25: Finding the Mechanism of Nb3Sn Cavity Healing
Strain applied to cavity causes cracks in Nb3Sn coating.
Somehow the recoating can repair cracks.
  Are the cracks being filled in?
  Is the Nb3Sn coating re-dissolving?
  Is the new Nb3Sn stoichiometric?
Nb3Sn coated wires are used to study crack formation and healing.
  0.1% to 0.5% elongation of the wire causes crack formation.

## Slide 26: Results of Wire Study
New Nb3Sn is formed in the crack and at the base of the crack in the Nb substrate.
New material is stoichiometric.

## Slide 27
Eric Viklund
Research Proposal:
SRF Cavity Manufacturing Cost Reduction

## Slide 28: HF-Free Bipolar Electropolishing
The use of HF in the fabrication of niobium SRF cavities provides a challenge for the large-scale production of cavities.
  Environmental impact of large volumes of toxic chemicals used.
  Human safety risk of working with toxic chemicals.
  Increased costs due to strict safety requirements and procedures.
Cost estimates for electropolishing with HF is $2,934 per cavity.1
1. Taylor, E. J., et al. SRF2015, Whistler, BC, Canada (2015): 359.
Bipolar electropolishing is a new technique for polishing niobium without using HF acid.
Material removal is achieved by alternating the polarity of the niobium.
  Anodic oxidation pulse
  Cathodic dissolution of the oxide
Bipolar electropolishing can utilize HF-free electrolytes or even neutral salt-based electrolytes.

## Slide 29: Bipolar Electropolishing Study
Bipolar EP has been shown to be effective by Faraday Technology, Inc., Cornell SRF group, KEK, and Jefferson Lab.
To integrate bipolar electropolishing in large-scale cavity fabrication for the ILC the removal rate must be improved.
  120 hours to remove 64 μm1
Removal rates are currently limited by the power supply.
  High currents during voltage pulse
  Electrolysis during cathodic pulse
  Limited repetition rate
F. Furuta et al., in Proc. 18th Int. Conf. on RF Superconductivity (SRF'17), Lanzhou, China, July 2017, paper TUPB074, pp. 567-570, ISBN: 978-3-95450-191-5, https://doi.org/10.18429/JACoW-SRF2017-TUPB074, 2018.
Tian, Hui, et al. No. JLAB-ACC-18-2836; DOE/OR/23177-4574; TUPO043. Thomas Jefferson National Accelerator Facility (TJNAF), Newport News, VA (United States), 2019.

## Slide 30: Plan of Study
Optimize bipolar EP parameters through a sample study
  Optimize pulse waveform for high efficiency
  Explore different electrolytes, neutral salt electrolytes
Electrochemical impedance spectroscopy will be used to analyze the electrochemical nature of the process to better determine the optimal pulse voltage and duration.
Utilize KEK’s vertical EP capabilities and develop high current pulsed power supply to perform bipolar EP on 1-cell and 9-cell cavities.

## Slide 31: Questions